STRENGTH OF MATERIALS I

Homework 4, Deadline: 4th of January 2012

QUESTION 1. For the beam model whose dimensions are given in the figure

- Draw the shear and moment diagrams.

- Determine the maximum bending stress that occurs on the critical section.

QUESTION 2. The beam carries a uniformly distributed load of w = 100 kN/m. The allowable tensile stress value for the material is 90 MPa and the allowable compressive stress value is 300 MPa.

- Define the critical section by considering the bending stresses and determine the bending moment on this critical section.

- Show whether the beam can carry this loading safely or not.

QUESTION 3. a) Determine and draw the orientation of the neutral axis on the beam cross-section. b) Calculate the maximum tensile and compressive stress values that appear on the cross-section.

QUESTION 4. The composite beam made of two steel straps and a wooden core is shown in the figure. If the allowable stress values for the wood and the steel are (allow)w  = 20 MPa and (allow)st = 130 MPa, then determine the maximum bending moment, M that can be applied to the beam. (Ew = 11 GPa, Est = 200 GPa).

# Text boxes

20 kN.m

45(